1.0	PURPOSE

This procedure describes a method for determining the day time visibility of pavement markings.

- 2.0		REFERENCES

- Nil.

- 3.0		DEFINITIONS

Nil

4.0		APPARATUS AND MATERIALS

- 4.1		Apparatus

Equipment as required for measurement of wear by Image Analysis, in accordance with TP904.

Equipment as required for measurement of luminance factor, in accordance with the relevant clauses of the appropriate 4049 Series standard.

4.2		Materials

- Nil.

5.0		SAMPLING AND SAMPLE PREPARATION

- Nil.

6.0	PROCEDURE

- 6.1	Intersection Markings

6.1.1	Drive through the intersection and assess the visibility of all markings using the parameters in Table 1. This assessment shall be carried out in daylight hours, when the pavement is dry, and under clear conditions. Roads which run essentially east- west shall also be assessed driving into the sun in the post-dawn and/ or pre-dusk period as appropriate.

6.1.2	If arrow recognition is an issue, it is likely that wear or contamination is the cause. Measure the degree of wear of the offending markings, in accordance with TP904, using a digital photograph of the entire marking. If the percentage of area intact is greater than or equal to 70%, then it is likely that contamination is the primary cause.

| Marking | Property | Assessment |
| --- | --- | --- |
| Arrow | Recognition | Is the directional requirement obvious at 60 metres? |
| Stop-bar | Visibility | Is the stop-bar clearly visible at 60 metres? |
| Pedestrian Crossing | Visibility | Is the pedestrian crossing clearly visible at 60 metres? |
| Turning lines | Visibility | Is the path required through the intersection clearly marked? |

Table 1 – Performance Parameters, Visibility at Intersections

6.1.3	Measure the luminance factor of the offending markings, in accordance with the relevant clauses of the appropriate AS 4049 series standard. If the luminance factor is less than 45%, then it is likely that contamination is the reason for the poor visibility.

6.1.4	If visibility is an issue with stop-bars, pedestrian crossings or turning lines, it is likely that wear or contamination is the cause. Measure the degree of wear of the offending markings, in accordance with TP904, using a digital photograph of the entire lane width of the marking, or individual bars of pedestrian crossing or turning lines. If the percentage of area intact is greater than or equal to 70%, then it is likely that contamination is the primary cause.

6.1.5	Measure the luminance factor of the offending markings, in accordance with the relevant clauses of the appropriate AS 4049 series standard. If the luminance factor is less than 45%, then it is likely that contamination is the reason for the poor visibility.

6.1.6	Record all measurements on Form TP945-1.

- 6.2	Line Marking Monitoring

6.2.1	Drive the section of road and assess the visibility of all markings using the parameters in Table 1. This assessment shall be carried out in daylight hours, when the pavement is dry, and under clear conditions. Roads which run essentially east west shall also be assessed driving into the sun in the post-dawn and/ or pre-dusk period as appropriate.

The vehicle speed used shall be the maximum posted speed for that section of road. The preview and assessment distances assume a straight and level road. No-overtaking and double barrier markings shall be visible at the distances specified for edge line, except where line of sight or line length is less than the specified distance.

| Speed, km/h | Preview Distance, m | No. of Stripes Visible | Length of Edge Line Visible, m |
| --- | --- | --- | --- |
| 40 | 55 | 5 | 55 |
| 50 | 70 | 6 | 70 |
| 60 | 83 | 7 | 83 |
| 70 | 97 | 8 | 97 |
| 80 | 111 | 9 | 111 |
| 90 | 125 | 10 | 125 |
| 100 | 139 | 12 | 139 |
| 110 | 153 | 13 | 153 |

Table 1 – Preview Distance Versus Speed

6.2.2	Record all measurements on Form TP945.

6.2.3	A number of locations over the length of a road may be tested such that an overall assessment can be made of the actual day-time visibility.

- 7.0	CALCULATIONS

- Nil.

8.0	PRECISION

- No precision data available at this time.

- 9.0	REPORTS AND DOCUMENTATION

- 9.1	Reports

- Nil.

- 9.2	Documentation

Form TP945-1.

Department of Planning Transport, Energy & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

Procedure – Laboratories

- Determination of Day-time Visibility of Pavement Markings

- TP945

| Test Program |  |
| --- | --- |
| Location |  |
| Date of Test |  |

Intersection Markings

| Marking Type | Location | Visibility/ Recognition | % Area Intact | Luminance Factor, % |
| --- | --- | --- | --- | --- |

Line Marking

| Marking Type | Visibility | % Area Intact | Luminance Factor, % | Comments |
| --- | --- | --- | --- | --- |

Recorded By:

- Checked By :

Form TP945-1, Revn. 2.7