- 1.0	PURPOSE

This procedure describes the methods to be used to audit line marking product, in terms of retroreflectivity, delineation and durability for DTPTI.

- 2.0	SCOPE

- These instructions pertain to the application of line marking by machine.

- 3.0	REFERENCES

TP907, Determination of Retroreflectivity of Pavement Markings

TP945, Determination of Day-time Visibility of Pavement Markings

4.0	DEFINITIONS

Line marking refers to the use of paint and glass beads as longitudinal marking.

A road section is defined as a length of road joining two towns or linking two or more significant roads.

- 5.0	PROCEDURE TO BE FOLLOWED

5.1	Sampling Plan

The aim of this procedure is to assess the effectiveness and consistency of application of line marking, against established requirements. Test sites will be selected on the basis of substrate, location, road category and marking schedule. A sampling plan shall be prepared prior to commencement of testing, to ensure that the sample is representative of the area to be evaluated. Retroreflectivity sampling plan shall be developed using the following rules:

- A rural road length is deemed to be joining 2 towns or significant centres.

- A metropolitan road length is the full extent of a road within the confines of a marking zone.

- For short test sections such as plant certification or process audit sites, a single set of measurements shall be taken in accordance with TP907.

- For road lengths of up to 20 kilometres, a minimum of 3 sites will be tested.

- For road lengths of 20 to 30 kilometres, a minimum of 4 sites will be tested.

- For road lengths of up to 30 to 50 kilometres, a minimum of 5 sites will be tested.

- For road lengths of 50 to 100 kilometres, a minimum of 6 sites will be tested.

- For road lengths of greater than 100 kilometres, testing will be carried out at maximum intervals of 20 kilometres.

- All testing shall be carried out in accordance with TP907.

- Testing shall be carried out on all lines at each location, including centre, separation, edge, single and double barrier.

Details of test locations shall be recorded. Where repeat testing is to be carried out at the same location, such locations shall be marked on the pavement.

  - Auditing

5.2.1	Audits shall be carried out as per Table 1, by Surveillance Officers or Technical Services Group personnel.

    - Determine the accuracy of placement and dimensions of markings, and for new work, the placement relative to spotting or marking out. The tolerances for line marking shall be as detailed in Table 2.

    - Assess marking for the presence of pick-up. If pick-up is evident the Contractor shall obliterate any "re-distributed paint" caused by vehicles passing over uncured work by removing and/or covering the "re-distributed" paint with a treatment of appropriate colour and type to match the existing road surface. Where the initial retroreflectivity measured within 10 days of application using a calibrated MX 30 reflectometer is below 240mcd/m2/lx, the markings shall be deemed to have been damaged because of inadequate protection, and the Contractor shall repaint the offending pavement marking.

    - Carry out an assessment of day-time visibility in accordance with TP945, at locations as per the sampling plan.

    - Carry out retroreflectivity measurement in accordance with TP907, at locations as per the sampling plan. Determine the date marked and calculate the exposure period. Using the chart in Appendix 1, determine the minimum value for the exposure period and road traffic volume. Average values below the minimum, at a specific test location, indicate non-compliance. Non-complying marking will be deemed to extend to the nearest complying location in each direction, for the purposes of Corrective Action.

Note:  	The values shown in the Appendices relate to measurement with an MX 30, calibrated to traceable CIE standards.

Any results found to be outside of specified requirements shall be treated as non-conformance, and shall be managed in accordance with the Pavement Marking Quality Plan.

Table 1 – Audits

| Criteria | Data Source | Action |
| --- | --- | --- |
| Placement, new markings | Relative to spotting | Measure/ Document |
| Placement, maintenance markings | Relative to existing markings | Measure/ Document |
| Dimensions | Stripe/ Module length | Measure/ Document |
| Pick-up | Visual | View/ document |
|  | Measured | Measure |
| Retroreflectivity | Visual | View/ document |
|  | Measured | Measure |
| Day-time Visibility | Visual | View/ document |

Table 2 – Placement/ Dimension Tolerances

| Type | Detail | Requirement |
| --- | --- | --- |
| New Work | Spotting | 50mm from seal centre |
|  | Lateral deviation | 25mm from spotting |
| New/ Maintenance | Stripe width | +10 -0mm |
|  | Stripe length, <12m | +150 -0mm |
|  | Stripe length, >12m | +300 -0mm |
|  | Module length, 12m | +150 -0mm |
|  | Module length, >12m | +300 -0mm |
|  | Edge parallel to centre | 25mm |
|  | Lane width | +50mm -50mm from correct width |
| Maintenance | New over old, lateral | <10mm |
|  | New over old, longitudinal | +150 -0mm |

- 6.0 	DOCUMENTATION

- Complete form TP950

Department of Planning, Transport & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

- Procedure

- Audit – Line Marking Product

- TP950

- Audit No.:……………………………………………………………………………………..

Date of audit:     /     / 	 Date Marked:     /     /  	Exposure Period :…………….

| PLACEMENT |  |  |  |  |
| --- | --- | --- | --- | --- |
| New Work | Spotting |  | Lateral deviation |  |
| New/ Maintenance | Stripe width |  | Stripe length, <12m |  |
|  | Stripe length, >12m |  | Module length, 12m |  |
|  | Module length, >12m |  | Edge parallel to centre |  |
|  | Lane width |  |  |  |
| Maintenance | New over old, lateral |  | New over old, longitudinal |  |

| RETROREFLECTIVITY |  |  |  |  |
| --- | --- | --- | --- | --- |
| Location |  |  |  |  |
| Visual assessment |  |  |  |  |
| Exposure Period, days |  |  |  |  |
| Result, mcd/ m2 /lx |  |  |  |  |
| Target, mcd/ m2 /lx |  |  |  |  |

Comments :……………………………………………………………………………………………..

……………………………………………………………………………………………………………

……………………………………………………………………………………………………………

Testing Officer:.........................................………………………………………………....……….

Form TP950-1, Revn.2.5

# Appendix 1

Department of Planning, Transport & Infrastructure

19 Bridge Road, Walkley Heights, Ph (08) 8260 0230, GPO Box 1533, Adelaide SA 5001

Technical Services Group

- Procedure

Retroreflectivity Requirements

| Roads with >10000 vehicles/ day |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Days of Wear | 0 | 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 |  |  |
| Retroreflectivity, mcd/m2/lx | 275 | 240 | 205 | 185 | 175 | 165 | 145 | 125 | 120 |  |  |
| Roads with 4000 to 10000 vehicles/ day |  |  |  |  |  |  |  |  |  |  |  |
| Days of Wear | 0 | 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 |
| Retroreflectivity, mcd/m2/lx | 275 | 240 | 205 | 195 | 185 | 175 | 165 | 155 | 145 | 135 | 120 |
| Roads with 1000 to 4000 vehicles/ day |  |  |  |  |  |  |  |  |  |  |  |
| Days of Wear | 0 | 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 |
| Retroreflectivity, mcd/m2/ lx | 275 | 240 | 225 | 225 | 220 | 220 | 215 | 215 | 200 | 195 | 190 |
| Days of Wear | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 |  |  |
| Retroreflectivity, mcd/ m2 / lx | 185 | 180 | 175 | 170 | 165 | 155 | 145 | 135 | 125 |  |  |
| Roads with <1000 vehicles per day |  |  |  |  |  |  |  |  |  |  |  |
| Days of Wear | 0 | 20 | 60 | 100 | 140 | 180 | 220 | 260 | 300 | 340 | 380 |
| Retroreflectivity, mcd/m2/ lx | 275 | 265 | 255 | 240 | 240 | 235 | 235 | 230 | 230 | 225 | 225 |
| Days of Wear | 420 | 460 | 500 | 540 | 580 | 620 | 660 | 700 | 740 | 780 | 820 |
| Retroreflectivity, mcd/m2/ lx | 220 | 220 | 215 | 215 | 210 | 210 | 200 | 200 | 190 | 190 | 170 |
| Days of Wear | 860 | 900 | 940 | 980 | 1020 | 1060 | 1100 |  |  |  |  |
| Retroreflectivity, mcd/m2/ lx | 170 | 150 | 150 | 145 | 140 | 130 | 120 |  |  |  |  |

Note:	The values shown above relate to measurement with an MX 30			reflectometer, calibrated to traceable CIE standards, and take account of 	the uncertainty of measurement as stated in TP907.

Form TP950-2, Revn. 2.5